## Slide 1: Looking Inside the Organic Solar Cell: Surfaces and Interfaces
S. Ismat Shah
Physics and Astronomy
Materials Science and Engineering
University of Delaware
Tbilisi State University, July 2014

## Slide 2: Hashimoto Predictions
Notes: Kyoto University

## Slide 3
Hashimoto Solution

## Slide 4: 95% Renewable Energy World

## Slide 5
Notes: Plextronics, Inc. 2180 William Pitt Way Pittsburgh, PA 15238 Phone: (412) 423-2030 Fax: (412) 423-2039

## Slide 6
DSSC
OSC
QDSC
OTSC
Provoskite
Notes: OTSC = Organic tendam cell

## Slide 7: Conjugated Polymers: (Semi)conducting behavior
Double and single bond provide the semiconducting properties
2s 2p3
sp3 hybrid
2s
2s
sp2 hybrid
2s 2p2
pz unhybridized
2p
x y z
x y z
+
π-bond
σ-bond
Notes: Q: what is the single double configuration i.e. is it pi sigm, pi sigma repetition?

## Slide 8: Two conditions to become conductive:
The first condition for this is that the polymer consists of alternating single and double bonds, called conjugated double bonds.
Every bond contains a localized “sigma” (σ) bond which forms a strong chemical bond. In addition, every double bond also contains a less strongly localized “pi” (π) bond which is weaker.
Conducting Polymers

## Slide 9
The second condition is that the polymer has to be altered - either by removing electrons from (oxidation), or inserting them into (reduction), the material.
1-Oxidation with halogen (or p-doping).
2- Reduction with alkali metal (n-doping).

## Slide 10: Conducting Polymer Inventors
Notes: 2000 Chemistry Nobel Prize

## Slide 11: What is organic semiconductor?
Organic semiconductor
LUMO: lowest unoccupied molecular orbital
HOMO: highest occupied molecular orbital
Inorganic semiconductor & metal
CB: conduction band VB: valance band
F. Gutmann, “Organic semiconductors”, Wiley, New York, 1967.
N = 1 2 4 …. Polymer Si,Ge… Metal
Energy
LUMO
CB
VB
VB
CB
HOMO
HOMO
LUMO
EG
(Number of
molecules)
π*
π
Notes: Increase number of monomer unit.
Extend conjugation  lower Eg (HOMO higher, LUMO lower)
High conductivity in Metal  easily move

## Slide 12
Difference in PV Mechanisms
Inorganic PV
Organic PV
Anode
hole
e-
Light
Input
-
+
Cathode
n-type
p-type
-
-
-
+
+
+
+
-
hole
e -
e- Donor
―
+
Cathode
Anode
e-
Acceptor
Exciton
―
+
Light
Input
Interface
Angew. Chem. Int. Ed. 47, 58 (2008)
Screening and Dielectric Constant
Notes: p-n junction  depletion zone

## Slide 13
Bulk-heterojunctions
Excitons binding energy in organic materials is 0.4~0.5eV
Bulk-heterojunction: Blend of two materials with different electron affinity and ionization potential (electron donor and acceptor)
diffusion length ~10nm
Exciton dissociation at the interface by the local field
provide more interface
–
+
–
+
Bulk heterojunction
e- Acceptor
e- Donor
D+A D*+A
D*+A [D*,A]
[D*,A] [D+*,A-*]
[D+,A-*] D++A-
1- Photo-excitation
2-Excitons diffusion
3-Tranfer (geminate pair)
4- Charge separation
hυ
Angew. Chem. Int. Ed. 47, 58 (2008)
Notes: Typically the exciton binding energy is of the order of 10±6 meV for common inorganic semiconductors. In organic materials it can be 1 eV.

## Slide 14: Selected materials for organic solar cells
Molecular structure and conjugated π-electron system
Ref. McMurry, J., Organic Chemistry. 3rd ed.; Brooks/Cole Publishing Company: 1992. and Angew. Chem. Int. Ed., 47, 58 (2008)
(b)

## Slide 15: Enhancing OPV Performance
Light Absorption:
New Materials
Using Plasmon Effect
P3HT Crystallization
Exciton Diffusion:
Heterogeneous structure
A-D Interface
P3HT Crystallization
Charge Separation:
A-D selection
C-nanotubes
Addition of oxide nanoparticles
P3HT Crystallization
Charge Extraction:
Reduce parasitic resistance
New contact designs
ZnO Nanowires
Al-active layer interface
P3HT Crystallization

## Slide 16: Bulk Heterojunction
Our research focuses on poly(3-hexylthiophene) and [6,6]-phenyl C61-butyric acid
Methylester blends

## Slide 17
P3HT Crystallization
b=0.38 nm
Adv. Funct. Mater. 2005, 15, 1193-1196
Chart: Degrees (2 Theta)
Chart: Annealing Temperature (degrees Celsius)
| 30 | 60 | 80 | 100 | 120 | 140 | 160 | 180 | 30 | 60 | 80 | 100 | 120 | 140 | 160 | 180
XRD Crystallite Size | 351 | 472 | 471.6667 | 734.6667 | 690.6667 | 718.6667 | 972.6667 | 480.3333 | 449 | 448 | 588 | 579.6667 | 683 | 791 | 876.6667
Annealing P3HT increases the crystallinity, which also increases the carrier mobility leading to overall increased device performance
Bakhtyar, Murray and Shah, JAP 2012

## Slide 18: JV Analyses
Voc, Jsc, FF, and PCE are all traditionally extracted from JV curves
As Cast:
After Annealing:
Murray, Shah et al., J. Photon. Energy 3(1), 032098 (2013)

## Slide 19: Annealing Effects
Chart: Annealing Temperature (C )
| 25 | 60 | 80 | 100 | 120 | 140 | 160 | 180
Efficiency | 0.36 | 0.56 | 0.7 | 1.19 | 1.55 | 1.85 | 2.44 | 2.4
Voc | 0.4792 | 0.4462 | 0.4263 | 0.4751 | 0.5023 | 0.5699 | 0.6239 | 0.6409
Jsc | 1.501 | 3.176 | 4.041 | 6.087 | 7.462 | 6.716 | 7.264 | 6.705
As Cast:
After Annealing:
Murray, Shah et al., J. Photon. Energy 3(1), 032098 (2013)

## Slide 20: Photocarrier Physics
Simple model of a lumped circuit diagram conveniently and accurately describes most solar cells, including OPVs
Notes: G is the generation rate

## Slide 21: Differentiation of JV
G = Shunt conductance
q = Electron charge
J0 = Diode saturation current
A = Diode ideality factor
k = Boltzmann’s constant
T = Temperature
V = Voltage
If dJ/dV is relatively flat, the y-intercept = 1/Rshunt
Murray, Shah et al., J. Photon. Energy 3(1), 032098 (2013)

## Slide 22: Differentiation of JV
Slope = q/AkT, Intercept = Jo
Murray, Shah et al., J. Photon. Energy 3(1), 032098 (2013)

## Slide 23: Device Resistances
Upon annealing, both series and shunt resistances respond favorably
Chart: 
| 30 | 60 | 80 | 100 | 120 | 140 | 160 | 180
Series Resistance | 84.2008 | 61.2542 | 62.1137 | 44.1787 | 18.7103 | 14.9245 | 23.2623 | 22.5063
Chart: Shunt Resistance
| 180 | 160 | 140 | 120 | 100 | 80
 | 2321 | 2352 | 1499 | 1098 | 379 | 61
Murray, Shah et al., J. Photon. Energy 3(1), 032098 (2013)

## Slide 24: Circuit Parameters
The dark saturation current and the diode parameter, both measure of recombination, decreased
Chart: Diode Parameter
| 180 | 160 | 140 | 120 | 100 | 80
 | 1.07 | 1.1 | 1.41 | 4.734 | 5.608 | 5.013
Chart: Dark Saturation Current "Jo"
| 180 | 160 | 140 | 120 | 100 | 80
 | 3.605e-05 | 6.896e-05 | 0.0002891 | 0.0002433 | 0.0009322 | 0.00098
Murray, Shah et al., J. Photon. Energy 3(1), 032098 (2013)

## Slide 25: R-Corrected JV Curves
Device | Jo (mA/cm2) | A | R (Ω-cm2) | JLo (mA/cm2) | Voc (mV) | Lc/D | Vfb (mV) | Jsc (mA/cm2) | FF (%) | μτ (cm2/V) | PCE (%)
Raw Data | - | - | - | - | 560 | - | - | 10.4 | 46 | - | 2.7
R, η corrected | 7.8×10-7 | 1.4 | 14 | 11.8 | 577 | 5.5 | 590 | 10.8 | 83 | 1.7x10-13 | 6.0
Bakhtyar Ali, Shah, et. al., JAP, 112, 114514 (2012)

## Slide 26: Finding the Limiting Carrier Mobility-Lifetime Product μτ
Lc =zero bias drift collection length
μτ = mobility-lifetime product
Vfb = flat band potential
D = active layer thickness
μτ has a weak dependence on T and a strong dependence on D
Chart: Limiting Carrier Lifetime Mobility Product
| 180 | 160 | 140 | 120 | 100 | 80
 | 3.6845e-13 | 3.4095e-13 | 2.7608e-13 | 2.4529e-13 | 1.8766e-13 | 9.0978e-14
Murray, Shah et al., J. Photon. Energy 3(1), 032098 (2013)

## Slide 27: P3HT-PCBM Interface

## Slide 28
Focus
Defocus (-Z)
Over focus (+ Z)
Z=-25µm
Z=-20µm
Z=-10µm
Z=-25µm
Z=-20µm
Z=-10µm
Z=-25µm
Z=-20µm
Z=-10µm
Z=-10µm
Z=-20µm
Z=-25µm
Z=-10µm
Z=-20µm
Z=-25µm
Z=-10µm
Z=-20µm
Z=-25µm
Z=0µm
Z=0µm
Z=0µm
P3HT annealed at 160 C
P3HT:PCBM (1:1) annealed at 160 C
PCBM annealed at 160 C
(a)
(b)
(c)
Transmission Electron Microscopy

## Slide 29
There are two modes in EELS
The Electron Energy-Loss Spectrum (EELS)
The Energy-Filtered image (EFTEM)
Incident high-kV beam
Secondary
Electron (SE)
Characteristic
X-rays
Visible
Light
Backscattered
Electron (BSE)
Auger
electrons
Absorbed
electrons
Electron-hole
pairs
Bremsstrahlung
X-ray
Inelastically
Scattered electrons (E0 - E)
Direct
Beam
Elastically
Scattered electrons
Specimen
Eo
Eo
When electron penetrates a specimen, it can either be elastically or inelastically scattered [1].
Magnetic prism
In-Column Filters: Zeiss Libra® 120 Plus at DBI [2]
[1] Williams, D. B.; Carter, B. Transmission electron microscopy;Springer: New York, 1996
[2] www.zeiss.com
The energy-loss events provide useful information about:
Chemistry—the bonding
Electronic structure—the nearest-neighbor atomic structure
Electron Energy Loss Spectroscopy (EELS)

## Slide 30
Electron energy loss spectroscopy (EELS) and EFTEM image
Incoming e - beam
Specimen
Eo
Energy filter
unit
EELS spectrum
Eo
Eo-E
An energy window
Image obtained by collecting electron with energy E,
energy filtered TEM (EFTEM)
Out going e – beam

## Slide 31
P3HT:  19 eV
PCBM:  25 eV
Plasmon peak positions
PCBM
Energy (eV)
window width 7 eV
window width 7 eV
P3HT
19 eV
25 eV
30 eV
window width 7 eV
Counts (arbitrary units)
Counts (arbitrary units)
12
24
36
48
60
72
84
Electron Energy Loss Spectroscopy (EELS)
PCBM
Plasmon peak is a Fingerprint
P3HT
PCBM

## Slide 32
EFTEM imaging
100 nm
19 eV with 7 eV slit width
100 nm
0 eV with 7 eV slit width
100 nm
30 eV with 7 eV slit width
100 nm
25 eV with 7 eV slit width
P3HT:PCBM (1:1) annealed at 160oC for 60 min
19 eV with 7 eV slit width
500 nm
Brighter regions correspond to P3HT rich domains
Similar morphology, i.e. P3HT fibril structure, is observed on a sample annealed for 20 min
[1] Rujisamphan N and Shah. et al. (ACS Surface and Interfaces, under review)

## Slide 33
19 eV with 7 eV slit width
19 eV with 7 eV slit width
Annealed at 160 oC for 20 min
Annealed at 160 oC for 60 min
100 nm
100 nm
8.0 Å
16.4 Å
3.8 Å
Substrate
1 monomer of P3HT
The average length of fibril is 705 nm
The average diameter of fibril is 152 nm
Nopporn and Shah, Solar Energy Materials & Solar Cells 109 (2013) 56–62
Electron Energy Loss Spectroscopy (EELS)/EFTEM

## Slide 34
Out-of plane XRD
Out-of plane XRD results
(020)
(a)
d-spacing value perpendicular to a P3HTfibril (16.4 Angstrom )
SEAD results
pi-pi stacking distance (3.8 Angstrom)
along the P3HT fibril
(a) A spun cast P3HT sample
Other techniques to determine the structure

## Slide 35
Chains orientation/packing in the P3HT fibril
8.07Å
Ordered chain
P3HT fibril
Shah I. et al. ACS, Appl. Mat. Int. under review, ACS (2014).

## Slide 36: Al – Active layer Interface

## Slide 37: Focused Ion Beam (FIB) Machine
FIB column
Gas Injection System (GIS)
CCD camera
& illumination
Inlens - Detector
SE -Detector
Airlock
SEM
FIB– Ga+ ion
sample

## Slide 38: Organic Photovoltaic Device
Shah and Nopporn, Adv. Energy Mat. 2013

## Slide 39
TEM Sample preparation with FIB
2µm
2µm
1µm
1µm
2µm
(a)
(b)
(c)
(d)
(e)
(f)
Pt
3µm
Trench
Trench
Sample after thinning
Milling through the bottom
and side wall
In-situ picking up the sample
Lifting sample up
Ga+
Pt
A lamella TEM sample: 50 nm thick
Detaching the lamella sample
Ga+ beam

## Slide 40: Crossection TEM of interfaces in OPV
Shah and Nopporn, Adv. Energy Mat. 2013
Unannealed
Annealed

## Slide 41: Crossection TEM of interfaces in OPV
Shah and Nopporn, Adv. Energy Mat. 2013

## Slide 42: Elemental map of the interfaces in OPV
Shah and Nopporn, Adv. Energy Mat. 2013

## Slide 43: Al Elemental Map (pixelated) and Measured Depth profile
Cramer, Shah, et. al. ACS (2014)

## Slide 44: Fick’s Second Law

## Slide 45
Work of Hailey Carmer, an undergraduate student in the group
D = 1.8 x 10-17 ± 6 x 10-18 cm2/s
White pixels represent Al and black pixels represent P3HT.
This image has dimensions 22.53 x 19.57 nm.
D (diffusivity) of (1.8 x 10-17 ± 6 x10-18) cm2/s for Al in P3HT:PCBM was determined.
Aluminum diffusivity in the active layer
Al mapping

## Slide 46: Predicting Jsc from EFTEM Images (TEM and EFTEM)

## Slide 47: TEM and EFTEM Image Analysis

## Slide 48
PCBM distribution analysis
electrode
Substrate
[1] Mackay et al, Soft matter (2012)
Our results
electrode
Substrate
Kiel et al., Soft matter (2012) [1]
Electrode
P3HT:PCBM
substrate
Distance from the Al interface (nm)
100
80
60
40
20
Electrode
P3HT:PCBM
substrate

## Slide 49: Light Absorption in the active layer
Use Beer-Lambert law to calculate absorption: I = I0 exp(-αx) (1)
We assumed a 90% reflection at the polymer-Al interface on the back layer, then repeated the absorption as the light reflected up the device.
White represents the areas of highest absorption, which correspond to P3HT sections.
P3HT has a much higher absorption in the visible range (1.7x105 as compared to 2.7x104 for PCBM).
Notes: Use Beer-Lambert law to calculate absorption: I = I0 exp(-αx) (1)
Where I is the transmitted light, I0 is the incident light, α is the absorption coefficient and x is the thickness of the layer in cm.
By taking I0-I, we find the amount of light absorbed by the layer, and thus the number of excitons generated in that area. We then pass I to the next layer down, where it becomes I0 and the process is repeated.
We assumed a 90% reflection at the polymer-Al interface on the back layer, then repeated the absorption as the light reflected up the device.
This created the map of absorption shown in Figure 3.
White represents the areas of highest absorption, which correspond to P3HT sections. P3HT has a much higher absorption in the visible range (1.7x105 as compared to 2.7x104 for PCBM). Shading in the lower areas is observed as the P3HT above absorbs a significant amount of light.
How did you get this? Did you use the measured quantum efficiency?
How did you set layer thickness?
Any reference for this?

## Slide 50: Jsc Prediction
Light Absorption
Current Generation

## Slide 51: Conclusions:
OPV is promising but there are several issues related to stability, mobility, etc., that still need to be worked out.
Simple lumped circuit model is useful for modeling OPV devices.
EELS/EFTEM can provide the details needed to study the P3HT and PCBM interface.
Simple diffusion models can provide information pertinent to diffusion on Al in the devices
EFTEM in combination with other techniques gives you a peak into the inside of OPV device which is useful for understanding the device behavior.

## Slide 52: Thin Films and Nanostructures Group

## Slide 55
Incident high-kV beam
Secondary
Electron (SE)
Characteristic
X-rays
Visible
Light
Backscattered
Electron (BSE)
Auger
electrons
Absorbed
electrons
Electron-hole
pairs
Bremsstrahlung
X-ray
Inelastically
Scattered electrons (E0 - E)
Direct
Beam
Elastically
Scattered electrons
Specimen
Eo
Eo
EELS and EFTEM
Low-loss region (50eV)
High-loss region (50 eV)
Counts (arbitrary units)
Energy (eV)
Zero loss peak (ZLP)
Plasmon peak

## Slide 56
Plasmon character for P3HT and PCBM

## Slide 57
Plasmon characteristic peaks from a device

## Slide 58
EFTEM images of P3HT:PCBM (1:1) annealed at 160 C for 60 min. (a) at 18 eV, (b) 20 eV, (c) 22 eV, (d) 24 eV, (e) 26 eV, (f) 28 eV, and (g) 30 eV, respectively
19 eV with 7 eV slit width
500 nm
P3HT fibrils

## Slide 59
Comparison crosssectional TEM images obtained from BFTEM and EFTEM
EFTEM
BFTEM

## Slide 60: J-V analysis: Background
Where Vj ≡ V-RJ
(c) Taking the derivative of eqn. (a)
w. r. t. “J “:
(J+JL)-1 For RG<<1; JL= Jsc
(b) Taking the derivative of eqn. in part (a)
w. r. t. “V “: assuming JL is constant
The intercept gives the value of Jo and the slope gives the diode factor A
Which gives the value of G in the reverse bias when plotted as
(d) From eqn. (a) one can have;
(a) Diode equation
Ref. Steven S. Hegedus, Prog. Photovolt. Res. Appl. 12, 155 (2004)

## Slide 61
JL(V) loss: J at the maximum power point is ~39% less than J at far reverse bias. Similarly J at Jsc is 13% less than JLo
Principle of superposition is not applicable
J(V) analysis: JL(V) losses
JL(V)-losses
Notes: Voltage dependence introduces significant losses and the principle of suppers-position is not applicable

## Slide 62: Outstanding Issues

## Slide 63: Typical OPV Number

## Slide 64: Two conditions to become conductive:
The first condition for this is that the polymer consists of alternating single and double bonds, called conjugated double bonds.
Every bond contains a localized “sigma” (σ) bond which forms a strong chemical bond. In addition, every double bond also contains a less strongly localized “pi” (π) bond which is weaker.
Conducting Polymers

## Slide 65
The second condition is that the polymer has to be altered - either by removing electrons from (oxidation), or inserting them into (reduction), the material.
1-oxidation with halogen (or p-doping).
2- Reduction with alkali metal (n-doping).

## Slide 66: Conducting Polymer Inventors
Notes: 2000 Chemistry Nobel Prize

## Slide 67: OPV Material

## Slide 68: Conjugated Polymers
The most important aspect of conjugated polymers from an electrochemical perspective is their ability to act as electronic conductors
Material which could combine the processibility, environmental stability, and weight advantages of a fully organic polymer with the useful electrical properties of a metal
All conjugated polymers have quasi-infinite system extending over a large number of recurring monomer units. This gives the materials a directional conductivity, strongest along the axis of the chain. The simplest possible form polyacetylene (CH)x
While polyacetylene itself is too unstable to be of any practical value, its structure constitutes the core of all conjugated polymers.

## Slide 69: Conjugated Polymers
a
b
c
Conjugated polymer structure: (a) trans- and (b) cis-polyacetylene, and (c) polythiophene
Notes: Conjugated polymers are organic macromolecules which consist at least of one chain of alternating double- and single-bonds. Due to the fact the π-orbitals of the alternating double-and single-bonds mesomerize the single and double bonds becomes similar character. This means that the pz-orbitals of the carbon atoms which forms the conjugated chain overlaps also over the single bonds. Thus π-electrons can be easier moved from one end of the polymer chain to the other. However, the remaining bond alteration (possibly by Peierl's instability) makes conjugated polymers to be only one-dimensional semiconductors. Like inorganic semiconductors they can be doped, to increase their conductivity extremely. For the discovery and development of such conductive polymers Alan J. Heeger, Alan G. MacDiarmid, Hideki Shirakawa received the Nobel prize in chemistry in 2000. The most simple conjugated polymer is polyacetylene, which consist only of a single chain of alternating single- and double-bonds.
Structure formula of Polyacetylene.
In principle one can construct any devices that are available from inorganic semiconductors, like diodes and transistors, also from conjugated polymers. The most advanced development in the last decade was that of light emitting devices from polymers like polyphenylvinylene (PPV), polyfluorenes (PF), and polythiophenes (PT), which are already on the market. Blended with Fullerene (C60) or its derivates, the polythiophenes are also most promising materials for photovoltaic application.

## Slide 70: Conclusions
OPVs have low carrier lifetime and short diffusion lengths
Crystallization of P3HT increases conductivity, but also increases domain size which leads to increased electron-hole recombination
Simple lumped circuit model accurately describes these issues and allows a glimpse into the internal workings of the devices
Model allows extraction of otherwise difficult to obtain data, such as barrier heights and the limiting carrier mobility lifetime product μτ