## Slide 1: Diversified application of corrosion resistant materials
Dr. Olga Tsurtsumia
Georgian Technical University

## Slide 2: Outlook
RCSR
The concept of corrosion
Materials and their application fields
Work already done
Work to be conducted

## Slide 3: Republic center for structure research
Founded in 1987
RCSR is one of the major materials research and teaching centers in Georgia. The Republic Center for Structure Researches in the Georgian Technical University is serving several institutions in Georgia with the full range of methods for structural investigations of solid materials.
25 scientist, professionals in different fields of materials science and electron microscopy
Prof. Elguja Kutelia

## Slide 4: RCSR of GTU
Materials science fields:
  Nano powders
  Liquid metals (Ga purification)
  Crystallography of twinning in crystals
  High temperature corrosion resistant alloys…
  Structural analysis:
    SEM
    TEM
    AES
    Microscopy…

## Slide 5: Projects in RCSR within the last 10 years
CRDF/GRDF
ISTC/UNTC
Rustaveli National Science Foundation
EU FP7
Joint and individual projects with German and US partners

## Slide 6: HT corrosion resistant materials
Various ferritic alloys with different compositions:
  Fe-Cr-Al-(RE)
  DADI
  P92 …

## Slide 7: The principle
The developed oxide scale protects the underling bulk against environmental attack
Metallic alloy
Oxide layer

## Slide 8: The environments:
Any aggressive ones:
  High temperatures (dry)
  High temperature steam
  S rich (acid)
  Cl rich
  Ash (basic)
  Others …
  Or combination…
Thermal-chemical!!!

## Slide 9: Possible materials:
Multy- or single component materials forming stable dioxides or other complex oxides or other scales on the top
  Cr2O3
  Al2O3
  SiO2
  …

## Slide 10: Application fields:
Since we deal with HT corrosion resistant materials:
    Power generation
    Automotive industry (catalytic converter )
    Some electrical devices
    Household techniques
    And now medicine!

## Slide 11: Examples of metallic implants used in medicine
Pins
Bone plates
Screws
Bars
Rods
Wires
Posts
Expandable rib cages
Spinal fusion cages
Finger and toe replacements
Maxillofacial prosthetics

## Slide 12: Examples :

## Slide 13: Dental implants (requirements)
Resistance against the corrosion attacks
Mechanical stability
Ability to be attached to the bone tissues in shortest time possible causing no or minimal inflammatory problems if possible
Price

## Slide 14: Existing materials for osseointegration:
Special types of steels
  austenitic 316 stainless steel
  martensitic 440 stainless steel
  martensitic 420 stainless steel
Ti and its alloys:
  Ti-6Al-4V

## Slide 15: Fe – Cr – Al alloy
It meets all of the requirements listed above
This drove us to the idea of trying our material in the radically different field, which is an osseo-implantology

## Slide 16: What our alloy offers:
Since the alloy we investigate produces extremely stable alumina of alpha modification, the metal itself is got covered with it completely, it can provide us with all the requirements listed above

## Slide 17: The self-organized ceramic layer
Which is Al2O3
Conditions for its forming is a high temperature above 1000OC

## Slide 18: Procedure of MCC
HydroxyApatite (HA) [Ca₁₀(PO₄)₆(OH)₂] is known as a typical representative of the biologically active ceramics the coatings if which on the implant materials is considered as one of the ways of achieving the natural and accelerated bonding to the living tissues.
Metallic alloy
Oxide layer
HA
Hydroxyapatite powder (a) and thermally
pretreated Fe-Cr-Al-RE alloy (b) using
Electrophoretic deposition technique.

## Slide 19: EBSD results
PM2000: Polished/
2000h/1100OC/air
AluchromYHf: Polished/
2000h/1100OC/air
Model alloy (with high Cr): 2000h/1100OC/air
↑ Alloy
↑ Alloy
↑ Alloy
Oxide ↓
Columnar
Equiaxial
Columnar
Fine-grained equiaxial
Fine-grained equiaxial
Fine-grained equiaxial

## Slide 20: Advantages of our material
    There are several strong advantages of Fe-Cr-Al alloy to be attractive for its further investigation in the direction of the implantology:
        Ability of the detail forming using any kinds of mechanical treatment: stamping, extrusion, cutting drilling …
        The alumina coating can be received all over the detail
        Non toxic (no contact of metal with human bones)
        HA coating is got not on the ceramic layer (not metal)
        Double protected (thus!)

## Slide 21: Work to be done
Optimization of HA deposition technique and the parameters of deposition itself
Improving the adhesion between two ceramics
Conducting:
    Mechanical tests
    Bio-chemical tests in simulated saliva and growing osteoblast cells
    Structural analysis
    Application of the same technology on the porous metals
    …

## Slide 22: Thank you for the attention!