## Slide 1: Wood Density Variation across Georgian Forests
Species Differences and Environmental and Stand-Structural Controls
98 plots
629 cores
13 species
Vasil Metreveli et al.
Ilia State University · Tbilisi, Georgia
Conference presentation · September 2026

## Slide 2: A 30-minute story in four steps
ROADMAP
TALK STRUCTURE
01
Why it matters
Wood density influences tree strategy, mechanical characteristics, biomass, and carbon.
02
How we measured it
98 NFI plots, 629 cores, 13 species, standardized field and laboratory protocol.
03
What varies
Strong species contrasts, smaller
stand-structural and environmental effects.
04
Why it matters for Georgia
Improved species-specific carbon conversion and geographical prediction.

## Slide 3
MOTIVATION
Wood density is a powerful forest trait
WHY IT MATTERS
WOOD DENSITY
ρ = m dry / V
A simple trait with multiple downstream consequences
Carbon accounting
Converts measured stem volume into dry biomass and carbon.
Tree strategy
Reflects structural investment, growth and hydraulic safety.
Wood quality
Related to strength, durability and potential uses.
Background: Chave et al. (2006); Pan et al. (2011); Mo, Crowther & Maynard (2024).

## Slide 4
CARBON LOGIC
FROM VOLUME TO CARBON
Species-specific density changes biomass estimates
Stem volume × wood density = dry woody biomass
0.42 g cm⁻³
Low-density species
≈ 420 kg dry mass per m³
0.64 g cm⁻³
High-density species
≈ 640 kg dry mass per m³
For the same stem volume, the difference is about 52% in dry mass.

## Slide 5: Georgia combines high forest diversity with changing environmental gradients
~45%
of the country is forested
4,598
First NFI plots
A natural gradient laboratory
Humid western forests, drier eastern landscapes, broad elevational ranges, and major transitions from deciduous stands to high-elevation conifers.
Study area and national inventory context: manuscript Introduction; MEPA (2023).
Wellenbeck et al., 2026

## Slide 6: The Caucasus remains underrepresented in wood-density datasets
KNOWLEDGE GAP
WHY THIS STUDY
Global resources exist
Despite unequal regional coverage and local calibration, large trait databases provide valuable species-level information.
Georgia-specific values are sparse
Previous work in the Caucasus is often species-specific or descriptive rather than national and environmentally explicit.
Carbon accounting needs local calibration
When local populations, species composition, and environmental factors differ, derived densities can transmit bias.
Manuscript Introduction: Zanne et al. (2009); Kattge et al. (2020); Chalatashvili et al. (2024).

## Slide 7: Four questions organize the study
OBJECTIVES
STUDY QUESTIONS
1
How much does wood density differ among Georgia’s major tree species?
2
How do tree size and long-term radial growth relate to wood density?
3
Which climate, soil and topographic variables explain additional variation?
4
How can these data support biomass, carbon and future spatial predictions?
Working expectation: species identity should dominate the signal, while structural and environmental factors refine within-species variation.

## Slide 8: Wide environmental gradients were sampled nationally
SAMPLING DESIGN
98 PLOTS
98
sample plots
629
increment cores
13
tree species
Selected from the First NFI to span western and eastern Georgia across climatic, elevational and forest-type gradients.
Accessible territory only; Abkhazia and the Tskhinvali Region/South Ossetia were excluded because access was not possible.

## Slide 9: Field sampling captured both species and size variation
FIELD METHODS
TREE SELECTION
1
Select species
Trees present in designated NFI plots
2
Cover size classes
Small, intermediate and large DBH
3
Core at 1.3 m
4.3 mm inner diameter borer
4
Record fresh data
Core length + fresh mass
5
Measure tree
DBH + height
Minimum sampled DBH: 8 cm · Standard coring height: 1.3 m · Total cores: 629
10
Field protocol: manuscript Methods, section 2.4.

## Slide 10: Wood density was measured from oven-dry mass and core volume
LABORATORY METHODS
DENSITY MEASUREMENT
1
Measure core
Length and fixed 4.3 mm diameter define cylindrical volume.
2
Dry to constant mass
105 ± 2 °C for 48–72
h.
3
Weigh immediately
Minimize moisture reabsorption after removal from oven.
4
Calculate density
Oven-dry mass divided by core volume.
ρ = oven-dry mass (g) / core volume (cm³)
Laboratory protocol follows Chave et al. (2006) and related wood-density methods.

## Slide 11: The same cores also provided long-term radial growth information
LABORATORY METHODS
TREE RINGS
1
Mount cores
Affix dried cores to wooden boards
2
Prepare surface
WSL Core Microtome; sanding when needed
3
Scan
1,200 dpi
high-resolution images
4
Measure rings
CooRecorder / CDendro; 0.01 mm precision
5
Summarize growth
Mean radial increment for each core
Quality control: incomplete outer rings from the sampling year were omitted before calculating mean radial increment.

## Slide 12: One response variable, multiple predictor domains
DATA STRUCTURE
PREDICTOR FAMILIES
WOOD DENSITY
Tree & stand
Age · DBH · height · mean/median radial increment · volume
Climate
CHELSA temperature and precipitation variables
Soils
Bulk density · pH · texture · N · CEC · organic carbon
Topography & space
Elevation · slope · aspect · roughness · TPI · plot effect
All predictors were complete for n = 629 observations in the analysis dataset.

## Slide 13: Predictor screening is essential before ecological interpretation
COLLINEARITY
CORRELATION STRUCTURE
Temperature block
Several CHELSA temperature metrics are strongly positively correlated.
Precipitation block
Multiple precipitation metrics carry overlapping information.
Terrain + soil
Topographic metrics cluster, while soil texture/chemistry show their own dependence structure.
Modeling implication: select representative predictors rather than fitting every correlated variable together.

## Slide 14: The analysis separates species effects from residual structural and environmental effects
1
Species baseline
Quantify mean density and uncertainty for each of the 13 species.
2
Structural controls
Test DBH and long-term radial increment within the broader model.
3
Environmental controls
Evaluate selected soil, climate and topographic predictors after collinearity screening.
4
Plot structure
Account for residual
plot-level differences and spatial clustering.
Generalized Additive Mixed Model (GAMM) was used for the analyses
GAMs are useful here because several ecological relationships are expected to be nonlinear rather than strictly linear.

## Slide 15: Species identity produces the clearest wood-density contrast
RESULTS
SPECIES DIFFERENCES
≈ 0.42 → 0.64 g cm⁻³
Points show species means with 95% confidence intervals; symbols distinguish normal vs non-normal distributions; letters indicate group comparisons.

## Slide 16: The species ranking forms three broad density groups
RESULTS
ECOLOGICAL RANKING
LOW
≈ 0.42–0.44 g cm⁻³
Abies nordmanniana Alnus incana / A. barbata Tilia begonifolia
Picea orientalis Pinus hamata
INTERMEDIATE
≈ 0.49–0.57 g cm⁻³
Castanea sativa Fagus orientalis
HIGH
≈ 0.59–0.64 g cm⁻³
Carpinus betulus Quercus imeretina Carpinus orientalis Quercus iberica Quercus macranthera
The ranking is more informative for carbon conversion than a single national average density.

## Slide 17: The observed ranking is consistent with major wood-strategy differences
INTERPRETATION
FUNCTIONAL CONTEXT
Gymnosperms in this dataset
Caucasian fir, Oriental spruce, and pine are low-density. Tracheid-based wood is commonly used for mechanical and hydraulic safety in cold or high-elevation conditions.
Angiosperms span a wider range
Deciduous trees range from light alder and linden to dense hornbeam and oak. Vessel-based wood provides more structural and hydraulic strategies.
Important: lineage does not fully determine density—species ecology and local environment still matter within each group.
Functional interpretation follows manuscript Introduction and Sperry et al. (2006); Mo, Crowther & Maynard (2024).

## Slide 18
APPLICATION
A species choice can shift biomass conversion by roughly half
CARBON ACCOUNTING
Same stem volume
1 m³
LOW DENSITY
≈ 420 kg dry mass
HIGH DENSITY
≈ 640 kg dry mass
Inventory implication
A single default density can systematically over- or under-estimate dry biomass when species composition varies.
Carbon implication
The error propagates directly into carbon stock estimates and reporting.
Management implication
Species-specific density values improve conversion tables and scenario calculations.

## Slide 19: Environmental and stand-structural effects are present—but modest
RESULTS
PARTIAL EFFECTS
Most fitted effects stay close to zero relative to
the large species contrast.
Partial-effect plots shown for mean radial increment, DBH, soil silt, TPI, annual precipitation and plot-level effects.

## Slide 20: Tree size and radial growth show weak, directionally interpretable trends
RESULTS
STAND STRUCTURE
Mean radial increment
The fitted effect trends slightly downward at higher
long-term radial increment, but the magnitude is small and uncertainty widens at the extremes.
DBH
The partial response is near zero at smaller diameters and becomes more negative toward very large DBH values.
Interpretation: denser wood may be associated with slower growth or different allocation strategies, but species identity remains the dominant axis.

## Slide 21: Soil, topography and precipitation refine the pattern rather than redefine it
RESULTS
ENVIRONMENTAL CONTROLS
Soil silt
A shallow U-shaped partial relationship; effect sizes remain close to zero.
Topographic position
A weak nonlinear response with a small peak around intermediate positions.
Annual precipitation
A slight positive tendency across the observed gradient, again with small magnitude.
The emerging picture is one of secondary environmental modulation around strong species-specific baselines.

## Slide 22: The emerging hierarchy of controls is clear—but the analysis is still being refined
1
Species identity
Large separation among species means; primary driver in the current results.
2
Tree / stand structure
DBH and growth make minor intraspecies changes.
3
Environment
Soil, topography and precipitation have modest partial effects.
4
Plot-level variation
Residual local differences remain and are represented in the model.
Interpret with appropriate caution
Some predictor ranges are sparsely sampled, which widens uncertainty.
Correlated environmental variables require careful selection.
The current partial-effect figure is preliminary and should be read as conditional association, not causation.
Species × environment interactions are an important next step.

## Slide 23: From measured cores to national trait and carbon products
OUTLOOK
NEXT STEPS
01
Finalize species models
Estimate species-specific effects and interactions with robust uncertainty.
NOW
02
Map current density
Predict wood density across forested Georgia from environmental rasters.
NEXT
03
Link to biomass
Combine local density with NFI, forest composition and
remote-sensing biomass.
NEXT
04
Explore climate scenarios
Assess how warming and precipitation shifts may alter density patterns and carbon estimates.
NEXT

## Slide 24: Three take-home messages
1
Species differences are large
Mean wood density spans roughly 0.42–0.64 g cm⁻³ across the 13 sampled species.
2
Secondary controls are modest
Tree size, growth, soil, topography and precipitation refine—rather than dominate—the pattern.
3
Local density improves carbon accounting
Georgia-specific values strengthen biomass conversion and future spatial modeling.
Thank you
Questions & discussion
Vasil Metreveli vasil.metreveli.1@iliauni.edu.ge
Acknowledgments
ECO.Georgia · GCF · BMZ · GIZ · MEPA · Ilia State University · field and laboratory teams
Selected references: Chave et al. 2006 · Pan et al. 2011 · MEPA 2023 · Mo et al. 2024